## Slide 1
Hayat Bennadji a, Krystle Smith a, Shaka Shabangu a,b, Mishal Shah a, Lei Deng a,c, and Elizabeth M. Fisher a
a Sibley School of Mechanical and Aerospace Engineering, bDepartment of Soil and Crop Sciences, Cornell University, Ithaca, NY, USA
c Xi’an Jiaotong University. Xi’an, 710049,China
Woody Biomass Pyrolysis: Bench-Scale Experiments and Modeling
CONCLUSIONS
Important gaseous and light volatile species have been identified and quantified, and the timing and of their production during pyrolysis has been determined. Heating conditions and particle sizes are similar to those in pyrolysis kiln.
Detailed kinetic model has been refined to reflect our reaction thermochemistry findings.
Mineral content of biomass strongly affects processing time and pyrolysis conditions
COMPARISON BETWEEN EXPERIMENTAL AND SIMULATED TEMPERATURE HISTORIES
EFFECT OF WOOD GRAIN DIRECTION
05/23/2018
One-dimensional,
Pressure-driven convection described by Darcy’s law,
Diffusion neglected,
Effective thermal conductivity includes radiation through pores,
Two kinetic mechanisms:
  4-species Park* mechanism
  ~30-species Corbetta mechanism
*W.C . Park, A. Atreya, H.R. Baum. “Experimental and theoretical investigation of heat and mass transfer processes during wood pyrolysis.” Combustion & Flame 157 (2010) 481-494.
**Corbetta, Frassoldati et al., “Pyrolyisis of centimeter-scale woody biomass particles: kinetic modeling and experimental validation, Energy and Fuels 48(11) 6492-6499, 2014
Wood
Tar
Gas
Intermediate solid
Char
kc2
kg2
kc
kt
kg
kis
Tars from poplar pyrolysis at Tgas = 375 °C
The GC/MS tar analysis indicates the presence of large quantities of oxygenated aromatic compounds (~30) such as phenols , methoxybenzenes and levoglucosan.
CHEMICAL COMPOSITION OF TARS
Syngas
Char
Convective Heating
Conduction and Pore Convection
Tars (Bio-oil)
particle holder,
before and
after pyrolysis
EXPERIMENTAL SETUP
Gas temperature | 375 °C, 418 °C, 464 °C
Duct Reynolds number | ~5000
Size and shape | Cylinders: d=1.9 cm; L=4 cm Spheres: 2.54 cm, 3.81 cm
Biomass types | Poplar, white pine heartwood, white pine sapwood, corn stover, potassium-doped wood
FUTURE WORK
Compare predictions to pilot-scale (kiln) data
  Products
  Completeness of pyrolysis
Investigate additional parameters (moisture content…)
The temperature history is characterized by two distinct events: the first an endothermic reaction, followed by an exothermic reaction.
DESCRIPTION OF THE NUMERICAL MODELS
ACKNOWLEDGEMENT
Funding provided by Yossie Hollander and the Fondation des Fondateurs
Tgas = 375 °C
Tgas = 418 °C
In the Cornell’s pyrolysis; large biomass particles will be processed. Thus, heat and mass transfer resistances are expected. Significant internal temperature gradients influence the solid conversion and the amount and composition of the products obtained. A good understanding of the interaction between chemical and physical mechanisms during the thermal degradation of thermally thick particles of wood is of fundamental importance, for optimizing the conversion process. Computational models have been developed and tested through single particle pyrolysis experiments with a known geometry and well-defined conditions. Our work has investigated effects of particle size, wood type, mineral content, temperature, and grain direction on pyrolysis rates as well as and product composition (tar, gas, and char yields). The computational model can now be applied to choose kiln operating conditions and predict yields.
INTRODUCTION
SPECIES YIELDS
2.54-cm spheres
3.81-cm spheres
Chart: Yield (% wt)
| CO | CO2 | CH4 | CH3OH | HCHO | HCOOH | CH3COOH
371.23 °C | 2.4657 | 5.5975 | 0.053589 | 1.0513 | 2.9519 | 0.66737 | 2.6008
422.7 °C | 3.2671 | 6.7958 | 0.36491 | 1.0402 | 2.951 | 0.60636 | 2.6404
467.5 °C | 3.7852 | 6.8179 | 0.55238 | 1.1248 | 3.0521 | 0.50201 | 1.7826
Chart: Yield (% wt)
| CO | CO2 | CH4 | CH3OH | HCHO | HCOOH | CH3COOH
378 °C | 3.437 | 6.9807 | 0.020239 | 1.4782 | 3.3816 | 0.97204 | 2.062
417.15 °C | 3.4442 | 7.035 | 0.22056 | 1.6455 | 3.2596 | 0.87646 | 1.7263
464 °C | 3.7936 | 7.3721 | 0.41001 | 1.6094 | 3.7228 | 0.60055 | 1.53
COMPARISON BETWEEN EXPERIMENTAL AND SIMULATED SPECIES PROFILES
EFFECT OF MINERAL CONTENT
 | Parallel grain | Cross grain
Side view |  | 
Top view |  | 
1
418 C
374 C
Chart: TIME, min
Chart: TIME, min
464 C
Chart: TIME, min
EXPERIMENTAL CONDITIONS
Kinetics of heat release are much faster for wood doped with KCl (blue, green) or K2CO3 (red) than for undoped wood (black).
0.00
0.05
0.10
0.15
0.20
0.25
0
400
800
1200
Production rate [mg/s/ginit]
Time [s]
CO
CO2
HCHO
CO
CO2
HCHO
0.00
0.05
0.10
0.15
0.20
0.25
0
400
800
1200
Production rate [mg/s/ginit]
Time [s]
CH3COOH
CH3OH
HAA
CH3OH
0.000
0.005
0.010
0.015
0.020
0
400
800
1200
Production rate [mg/s/ginit]
Time [s]
H2
CH4
HCOOH
H2
CH4
HCOOH
2.54-cm wood spheres at 368 C